# SAFE OPERATING PROCEDURE

Strip Heater

|  | DO NOT use this appliance unless you have had instruction and training in its safe use and operation. Teacher permission MUST be given to operate this appliance. |
| --- | --- |
| The risk of injury when using this machine is LOW |

## IDENTIFIED RISKS AND HAZARDS

Hazards that may be encountered when using the plastic strip heater include:

- burns from the plate of the heater or the workpiece

- fire from protective paper catching alight

- electrical faults

Burns can occur from touching hot metal parts on the heater. Use caution when handling the heater - especially when packing away after a bending operation.

## PRE-OPERATIONAL SAFETY

- Always check that the heater and its electrical cord are in good working order.

- Check all adjustments and settings carefully before commencing any heating

operation.

- Make sure the heater is turned off before making adjustments.

- The work area should be clean and free of equipment, rubbish and other obstacles.

- Set up the strip heater at the correct height for safe operation.

- Adjust the temperature correctly.  Consult labels for manufacturer’s suggestions.

OPERATING SAFETY PRECAUTIONS

- Ensure that the workpiece rests flat on the strip heater.

- Allow the heater to reach maximum temperature before applying the workpiece.

- Keep hands well away from the resting plate when the heater is operating.

- Never leave the heater unattended when turned on.

- Keep fingers away from the heater's resting plate whilst heating.

- Remove the plastic paper from both sides of the plastic along the bend line and mark the planned bend using a wax pencil or china marker on the top surface.

- Keep the heated edge on the outside of the bend, if possible, and don't force the bend.

- Overheating can cause bubbles along the bend area while bending when it is too cold results in a highly stressed, weakened bend.

- Thicker gauges (over 3.0 mm) may require heating on both sides by turning the sheet over periodically during the heating cycle.

- Forming jigs and clamps should be used for best results.

# Text boxes

PLACE A PICTURE OF YOUR MACHINE or TOOL HERE